## Slide 1: Ultra-high light yield scintillation crystals detector based on low-temperature CsI and SiPMs for CEνNS detection
孙希磊
IHEP
2024.05.08 西昌

## Slide 2: Outline
Introduction
Successes and Challenges
Ultra-high light yield solutions
Prototype detector performance
Potential for CEvNS
Other Potential Applications
Summary

## Slide 3: CEvNS
Theoretical prediction, about 50 years ago
Experimental confirmation, 2017
Akimovet al.,Science357, 1123–1126 (2017)

## Slide 4: The CEvNS Physics
Rich physics, Eν <50 MeV
Reactor monitoring
Neutrino Magnetic Moment
Supernova
WIMPs direct detection
SM precision tests (Weinberg-angle)
Sterile Neutrino Search
Constrain NSI parameters

## Slide 5: Signals of CEvNS
Nuclear recoil, ~ keVnr to 10’s of keVnr, like WIMPs
Cross section is large ~ 10-38 cm2, 2 orders larger than IBD
Akimov et al., Science 357, 1123–1126 (2017)
J. Link Science Perspectives

## Slide 6: Detection technology of CEvNS
ar5iv.labs.arxiv.org/html/1509.08767
Photons, Phonons, Electrons
The same as WIMPs

## Slide 7: Successes and Challenges
First successful CEvNS detector, CsI(Na)+PMT at RT
Diameter 11 cm, length 34 cm, mass 14.57 kg
LY ~40000 photons/MeV, 420nm
QE ~33%, ~13.3 p.e./keVee
QF ~8.8%, ~1.17 p.e./keVnr
Jonghee Yoo’ report

## Slide 8: Ultra-high light yield solutions
Low temperature CsI+SiPM+TPB solution
CsI, LY >100000 photons/MeV, 2.5 times better than CsI(Na)
SiPM, PDE 50%-60%, 2 times better than PMT
Expected ~50-60 p.e./keVee
TPB（WLS）
SiPM
CsI
Low temperature

## Slide 9: Pure CsI crystals
LY be significantly improved at LT
The brightest scintillator, 310-340 nm
QF>100% for alpha/gamma
QF for nuclear recoil/gamma 10%, 20%???
LY of CsI(Na), CsI(Tl) is reduced at LT
New Physics: Sae Mulli,Vol. 71, No. 5, May 2021, pp. 469475
IEEE TRANSACTIONS ON NUCLEAR SCIENCE, VOL. 37, NO. 2, APRIL 1990
RDTM (2018) 2:15

## Slide 10: TPB wavelength shifter
Shift 340nm to 420 nm, match the SiPMs sensitive spectrum
Performance is enhanced at LT
Widely used in liquid argon detectors
R Francini et al 2013 JINST 8 P09006

## Slide 11: SiPMs Performance
PDE 50-60% at 420 nm
DCR reduced by 7 orders, < 0.01 CPS/mm2 at 77K
Optical cross talk, acts as a photon amplifier
AFBR-S4N66P014M NUV-MT Silicon Photomultiplier
Alberto Gola FBK

## Slide 12: Prototype detector
CsI crystal 5x5x5 cm, 0.56kg, polished
Packaging with Teflon reflective film without TPB
SiPMs array, 5x5 cm, two end readout, with TPB
Cooling to 77 K with liquid nitrogen
Low temperature front-end amplifier circuit

## Slide 13: SiPMs array performance
SiPM and preamplifier run stably at low temperatures
Single photoelectron resolution is very good
Consistency of the two arrays is very good
DCR ~0.1 Hz/mm2 @35V bisa
Eur. Phys. J. C (2024) 84:440

## Slide 14: Waveform performance
Decay time ~1 µs, Pulse Width ~3 µs
Baseline width <5 mV
Eur. Phys. J. C (2024) 84:440

## Slide 15: Energy spectrum
Test with 241Am and 55Fe
Excellent energy resolution, fine structures are clearly visible
Eur. Phys. J. C (2024) 84:440

## Slide 16: Luminescence linearity
Excellent luminescence linearity, no drop down below 10keV
Significantly better than LaBr3, NaI:Tl
Nuclear Science and Techniques (2024) 35:23
Eur. Phys. J. C (2024) 84:440

## Slide 17: Influence of SiPMs Cross Talk and After Pulse
CT, AP significantly increasing the measured p.e. number
Internal CT, AP triples the number of p.e. at 37 Vbias
External CT 1.4 times the number of p.e. at 37 Vbias
Eur. Phys. J. C (2024) 84:440

## Slide 18: Influence of TPB
Photoelectrons number is doubled with TPB
Eur. Phys. J. C (2024) 84:440

## Slide 19: Light yield
The measured p.e. number increases significantly with increasing bias voltage, 30 to 122 p.e. /keVee
122.7 p.e./keVee, a world record
30.1 p.e./keVee, after CT subtract (50% PDE at LT?)
Eur. Phys. J. C (2024) 84:440

## Slide 20: Issue of SiPMs eCT coincidence events
Events rate of eCT coincidence is very high
5 orders larger than accidental coincidence of DCR
Big issue for low threshold detectors
Need do further study, single-ended readout, correlation with iCT
Eur. Phys. J. C (2024) 84:440

## Slide 21: Potentials for the reactorCEvNS detection
Eur. Phys. J. C (2024) 84:440
35 m distance to 4.6 GWth reactor
Threshold 2 p.e.
QF=0.06, DCR= 0.1 CPS/mm2, DCR dominant background,

## Slide 22: Potentials for the reactor CEvNS detection
35 m distance to a 4.6 GWth reactor
Threshold 2 p.e
If QF ~15%?, DCR~0.01?, better sensitivity
Good chance for reactor CEvNS observation
Preliminary
Preliminary
With 104 eCT coin

## Slide 23: Other Potential Applications
Dark matter searches, better than RT NaI(Tl), CsI(Tl)
Gamma ray spectrometer, no intrinsic BKG like LaBr3
UNIVERSITY OF CALIFORNIA, BERKELEY
Journal of Radiation Protection and Research 2018; 43(3): 85-96

## Slide 24: Summary
Rich physics with CEvNS, very challenging
Ultra-high light yield solution is proposed
The prototype detector works well
eCT issue need further study
Application potential remains to be developed
Good chance for reactor CEvNS detection

## Slide 25
Thank you for your attention!

## Slide 26: Summary
DOI: 10.1002/adma.202304938

## Slide 27
From Jing Liu