## Slide 1
Radon-222 Screening Capability and Research at SNOLAB
Dr Nasim Fatemighomi (she/her)
Staff Scientist
On behalf of SNOLAB Assay Group
2025/08/25
TAUP 2025, Xichang, China

## Slide 2
Introduction
222Rn progeny are backgrounds to low energy neutrino and rare-event searches
Emanates from material surfaces
Present in SNOLAB air 120 Bq/m3
  N2 is widely used as a cover gas to keep radon out of experiments
SNOLAB supports low level 222Rn screening at site using four different radon extraction boards
  Measure 222Rn concentration in ultra pure water (UPW), N2 and 222Rn emanation from materials
From Wikipedia

## Slide 3
Underground Radon Assay Systems
Water radon board (Refurbished in 2019)
Sensitivity: (1.5 10-14 g238U/gH2O equivalent (slides 5-8)
(DOI: 10.1016/j.nima.2003.10.103)
SNO+ mobile board (Refurbished in 2021)
Used primarily for N2 gas assays
Board emanation rate: 44 7 Rn atoms/day
A new radon trap was developed to enhance gas assay sensitivity (slides 9-16)
(DOI: 10.1016/j.nima.2025.170422)

## Slide 4
Surface Radon Emanation Systems
SNOLAB radon emanation board (built 2021)
High sensitive radon emanation measurement SNOLAB technical report:
(SNOLAB-STR-2022-001) - available on request
Chamber emanation rate: 4Rn atoms/day
Radon research and development
Emanation
Chamber
Radon Board
DEAP-3600 board (refurbished 2023)
The board emanation rate < 6 Rn atoms/day@90% CL
Testing new radon detectors
Spherical proportional counter

## Slide 5
Water Radon Assay System
Designed and built by the SNO collaboration (DOI: 10.1016/j.nima.2003.10.103)
Operated by SNOLAB and SNO+ to monitor 222Rn level of SNO+ cavity UPW and SNOLAB UPW plant
Water trap
Degassser
Trap A
Trap B
The SNO+ experiment
Water shielding (7000 tonnes UPW)

## Slide 6
Water Radon Assay System
Water trap (-60 C)
Degasser
Radon extraction board
H2O from SNO+ cavity/UPW plant (19 SLPM)
Water return to cavity

## Slide 7
V203: Between Acrylic Vessel and PMTs
Results are consistent with SNO times
SNOLAB UPW plant radon level is (2.40.7)g238U/gH2O equivalent
= (0.14 0.04) Rn atoms/L

## Slide 8
SNOLAB/SNO+ Gas Assay System
Originally designed for vacuum radon emanation measurement
Has been adopted to perform N2 gas assays (SNO+/SNOLAB gas systems and PICO-500)
Modified low radon emanation vapor trap
Gas system filled with N2

## Slide 9
Primary Trap Limitation for Gas Assays
Radon traps use porous materials to enhance trapping
Bronze wool highly efficient under high vacuum
Gas assay efficiency decreases with longer duration or >1 SLPM flow
Limited extracted gas volume constrains sensitivity
Need for traps with more porous material
S.M.A. Hussain MSc thesis (2022)

## Slide 10
Activated Charcoal Trap
Activated charcoal traps used for gas purification
  G. Heusser, et al. Appl. Radiat. Isot., 52 (2000)
Gas assays require both trapping & efficient radon release
Developed a portable activated charcoal trap to enhance radon trapping
  Nasim Fatemighomi et al: Nucl.Instrum.Meth.A 1076 (2025)
Used low background Calgon OVC 4 × 8 (coconut-based)
In-house nitric acid etching to remove ²³⁸U background
Radon emanation: 183 mBq/kg at room temperature
100μm
22 g trap

## Slide 11
Radon Calibration Source for Trap testing
A calibrating source was made using Nora Xp 5319 rubber floor tile
10cm
14 x 10 cm2 floor tiles
Calibration Can
Fit is based on²²⁶Ra-supported emanation and ²²²Rn outgassing from porous rubber tiles

## Slide 12
Trap Efficiency Test Set-up
N₂ flow through the source introduces radon atoms to trap
Charcoal cooled with LN₂–alcohol mix to trap radon
Radon released from charcoal trap by heating to 150 °C
Released radon were extracted using the radon board

## Slide 13
Trap temperature tuned by LN₂ ratio in LN₂-alcohol mix
Efficiency: The ratio of radon extracted from radon trap to radon introduced to the trap
The trap was tested up to 5 SLPM
The efficiency of the trap is 100% for temperatures between -100 C to -50 C
Efficiency versus Cooling Temperature

## Slide 14
Unlike bronze wool trap, charcoal trap is 100% efficient after one hour of assay duration
Charcoal versus Bronze Traps
Bronze wool data shown in slide 9…

## Slide 15
Charcoal Trap Sensitivity and Use
N2 assay sensitivity 90Bq/m3
  Bronze wool sensitivity: 3.3 mBq/m³
SNOLAB LN2 plant
Trap used to measure radon in N₂ systems, incl. SNOLAB LN₂ plant boil-off
SNOLAB International Dewar

## Slide 16
Portable Lucas cells with ZnS(Ag) coating
ZnS(Ag) scintillates with α particles → ideal for radon detection
Eighteen Lucas cell channels available
Radon Counting
2” diameter PMTs and CAEN electronics
2” diameter
4 μs window

## Slide 17
Enhancing Radon Counting
New Lucas cell
In-house ZnS(Ag)
SPC (a la NEWSG)
New low background Lucas cells were fabricated: 3 /day
R&D toward lower background ZnS(Ag)
Exploring small low background spherical proportional counters (SPC) for β sensitivity (Dr. Pierre Gorel)

## Slide 18
At SNOLAB radon assay systems used to measure radon in UPW, solid samples, and N₂ gas
Developed a low-background radon trap to improve N₂ gas assay sensitivity
Continuing research on radon trapping methods
  R &D for radon measurement in noble gases
R &D toward making low background radon counting systems
Summary and Future Work

## Slide 19
Acknowledgement
Research Students (SNOLAB/SNO+): Yusuf Ahmed, Juliette Deloye, Peter Qin, Justin Suys, Keegan Paleshi, Adil Hussain, Jerry Lu and Ariana Pearson
Scientific Support Team: Lina Anselmo, Steven Maguire, Sharayah Read and Deena Fabris