## Slide 1: Study of Li2MoO4 and Na2Mo2O7 crystals for 100Mo neutrinoless double beta decay search with cryogenic bolometers
Deyong Duan
State Key Laboratory of Particle Detection and Electronics (SKLPDE)
University of Science and Technology of China (USTC)
The XIX International Conference on Topics
in Astroparticle and Underground Physics
August 27, Xichang

## Slide 2: Outline
Motivation
LMO&NMO Low Temperature Properties
  Light yield
  Heat capacity
LMO Bolometer Test
USTC Lab Status
Summary

## Slide 3
3
and cryogenic phonon-scintillating bolometer
Physics goal: neutrinoless double beat decay ()
Lepton number violation
Majorana or Dirac particles
Neutrino mass
Asymmetry of (anti-)matter…
Light-heat dual-bolometer
Absorber = Scintillating crystal
Low energy threshold
Good energy resolution
Particle identification ( vs. )

## Slide 4: Why molybdate crystals
CUPID-Mo
High Q value (3034 keV) &
natural isotope abundance
AMoRE-I
CaMoO4
AMoRE-II
Li2MoO4
Li2MoO4
Li2MoO4
@Modane
@Canfranc
@Y2L
ZnMoO4 PbMoO4
CdMoO4 Na2Mo2O7
Li2MoO4 @LNGS
Li2MoO4 @CJPL

## Slide 5: LMO&NMO Low Temperature Properties
01

## Slide 6: Scintillation light properties
LMO test with laser 280 nm, peak at 510 nm, lower temperature, higher light yield
Low temperature test platforms with laser (10-300 K), laser 250-1700 nm
Spectrofluorometer
Excitation spectrum @10 K and emission spectrum
Intensity
NMO-355 nm
Intensity
/nm
NMO test with laser 355 nm, peak at 620 nm, lower temperature, higher light yield
/nm
LMO-280 nm
Intensity

## Slide 7: Heat capacity measurement
PPMS (Physical Property Measurement System, Quantum Design), 50 mK - 400 K
Heat capacity measurements of LMO and NMO from 200 mK - 2 K with PPMS, the results are consistent with the Debye model, ,
as a function of T2
Test platforms
14.3 mg LMO
32.3 mg NMO
Thanks SICCAS for the crystals

## Slide 8: LMO Bolometer Test
We constructed serval LMO bolometers and tested they performance
02

## Slide 9: LMO Bolometer
Copper frame cleaning
Bolometer assembly
Electrical connection
LMO bolometer design
Fixed on the cryostat
NTD/Heater gluing
Cleaning
Drying
Gluing
NTD & Heater
Electrical connect
Spring Plate

## Slide 10: Running state
Water shielding reduced the pile-up events
LMO Temperature
  Down to 20 mK
No shield
Water Shield
10 sec
Water shield
Water shield
Crystal
Copper
PTFE

## Slide 11: Data Processing
Decay time ~ 16 ms
Calibrated by 22Na
  FWHM = 21.5 keV@511 keV
  Baseline resolution ~ 3.54 keV
1.5 s
Pulse shape

## Slide 12: LMO Bolometer
For still high pile-up rate
  Use the LMO
  Reduce size to reduce pile-up
Temperature is about 20 mK
Pile-up reduced
Assemble
LMO
Glue points
30 s

## Slide 13: Data Processing
Decay time ~ 13 ms
  Pile-up rate is lower
FWHM= 7 keV@511 keV
0.511 keV
1.27 MeV
1.5 s
Pulse shape
preliminary
preliminary

## Slide 14: USTC Lab Status
03

## Slide 15: USTC Ground Lab Status
Oxford Triton 500@USTC, 2021
Running with water shielding, reduce pile-up
Notes: effective

## Slide 16: Ground Lab Gamma Flux
CZT(CdZnTe) detector unfolding method high flux backgrounds
Long decay time (hundreds ms) pile-up events shielding
arxiv.org/abs/2401.12034

## Slide 17: Radioactive Shielding
Two orders of magnitude. Material: Pb (Pb-210<100 Bq/kg), Cu
Three design options: 10 cm Pb, 10 cm Pb +2 cm Cu, 15 cm Cu
Thickness: 15 cm Cu = 10 cm Pb
G4 simulation
Height: 120 cm = 140 cm

## Slide 18: Shield Construction
Foundation construction
Shield design
15 cm thick Cu will be used as shield, about 5 tons
The construction of the copper shield was finished

## Slide 19: Summary
LMO and NMO are both attractive crystals, especially for 𝟎𝝂𝜷𝜷 search
Scintillation properties and Heat capacity of LMO/NMO crystals have been investigated experimentally at low temperature
R&D work on scintillating crystals’ low temperature characteristics, bolometer design and mK running, radioactive shielding, NTD-Ge and LD fabrication for CJPL.
Thanks!
NTD-Ge and LD fabrication
Post ID: #55 #381

## Slide 20: Backups
04

## Slide 21: Stream data processing software
Collect triggerless stream data, python-based visualization software
Exploit a matched filter, the Gatti-Manfredi optimum filter, to maximize the Signal Noise Ratio (SNR) and to get the information about the pulse-shape parameters